- Acoustic wall cladding description

- Range Lauder LINEA - Product reference 4.2.4

Wall cladding lot

## General

Wall cladding will be created using 4.2.4 panels product reference from the Lauder LINEA

range of the Laudescher brand, which are compliant with standard EN 14915

Solid wood panelling and cladding.

The cladding is mechanically fixed directly onto a separate framework, in accordance

with the manufacturer's recommendations and installation good practice rules.

The service will include the supply and installation of the panels, with or without acoustic materials, and a separate framework which the panels are attached to. The installation company will be responsible for the assembly and execution drawings together with all related services (cutting operations, blockouts, offcuts, internal and external corners, plinths, etc.) in accordance

with manufacturer recommendations.

## Description of acoustic wall cladding

Acoustic wall cladding will be of the following type:

Range: Lauder LINEA

Product reference: 4.2.4

Form: Linear

Total thickness: 55 mm

Slat section: 42 x 20 mm

Facing side: 42 mm

Slat thickness: 20 mm

Rear black wooden counter-slats: 34 x 45 mm

Spacing between slats: 43,71 mm

Average void area: 51%

Reaction to fire: B-s1,d0 / B-s2,d0 as defined in standard EN 13501-1

D-s1,d0 untreated wood  as defined in standard EN 13501-1

Solid wood:

- Pine

- Douglas Fir

- Oak

Finishing: (in accordance with building class)

- Clear varnish

- Wax Color

- Wax Color MC

Wax Color or Wax Color MC finishing on Pine, with the following choice available to contractors: Honey, Oak, White, Wenge, Cherry, Chocolate, Mahogany, Grey.

- Edging system: edge A

- Modular dimensions: 1880 x 600 mm and 1265 x 600 mm

## Acoustic recommendations

Any modification of recommended materials and the use of materials not covered by an acoustic test report (French or European) specifying their acoustic characteristics will be subject to the prior written agreement of the contractor. Extracts of commercial documents cannot under any circumstances

be used to replace acoustic test reports.

Acoustic performance will be achieved by adding mineral or stone wool tiles measuring 595 x 595 mm and 20 mm thick. They will have a minimum density of 100 Kg/m3. They will be faced with black fleece.

Tests will be conducted in compliance with standards EN ISO 354 and EN ISO 11654 on a plenum

of 50 mm.

## Fire recommendations

The product must be supplied with a test report performed on the finished product, in acoustic or open version, in an approved laboratory in accordance with standard EN 13501-1.

Reaction to fire: B-s1,d0 / B-s2,d0 as defined in standard EN 13501-1 report no. 12/RC-13

D-s1,d0 untreated wood  as defined in standard EN 13501-1

- Technical performance

- The products must have a VOC classification in accordance with EN ISO 16000-3, 6, 9 and 11

in compliance with current legislation

- PEFC / FSC: the product must be supplied with a certificate and individual number

- Humidity resistance: in accordance with building class

- Maintenance: keep free of dust. Lauder LINEA panels must not be cleaned with detergents

or water-based products under any circumstances

- Storage: products in the Lauder LINEA range must be stored flat, in premises with constant indoor humidity sheltered from water and blown air heating. Products in the Lauder LINEA range must be stabilised in the destination premises for at least 48 hrs prior to installation.

- Installation

- The panels are screw-mounted onto a separate grid at distance "D" of 615 mm, in line with

the recessed black wooden counter-slats of the panel (black screw heads or screws with black covers / 2 screws per counter-slat).

The system gives the panels a perfectly flowing and seamless appearance.